## Slide 1
Hollow plastic parts
Polymer Processing, BMEGEPTAGE3
Béla Zink, PhD, assistant professor
2021

## Slide 2
Hollow plastic parts:
One-piece product (not assembled) with a relatively thin wall; open or closed part/product
In the case of open geometry, the opening must not be larger than the cross section.
Size (volume) range 1-2 cm3 … 5(50) m3
Products with any shape can be prepared (spherical, flat)
From a couple of pieces to a couple of million pieces (series)
Process of hollow plastic parts:
Extrusion blow moulding
Injection blow moulding
Rotational moulding
Twin-sheet thermoforming
Gas or water-assisted injection moulding
Lose core injection moulding
Hollow plastic parts

## Slide 3
Extrusion blow moulding

## Slide 4
Extrusion blow moulding:
https://youtu.be/C2DQ8JudbBE
Forming of the extruded tube (parison) in a closed mould with compressed air to a hollow plastic part/product.
Major steps: parison production with a single screw extruder; blowing of the parison in the closed mould, cooling and ejection; flash removal.
Extrusion blow moulding

## Slide 5
Parameters of tube extrusion to be considered :
High melt strength of the selected polymer (and/or lower melt temperature): if it is lower, the tube will not carry its own weight, if it is higher, the parison cannot be formed
No weld lines on the parison (die design)
Uniform flow profile, uniform wall thickness (along the circumference of the parison). During shaping the melt in the die: shear and elongational deformation – molecular orientation – relaxation and swelling will occur (die design).
Uniform tube temperature: a warmer region will deform more than a colder region
The weight of the parison will load the parison itself – stretching – decreasing wall thickness.
Complexity of the product’s geometry (no sharp edges,
no big flat surfaces, max blowing index is 4:1,
wall thickness and volume relationship)
Extrusion blow moulding

## Slide 6
Due to different phenomena, changing the wall thickness along the length is recommended:
To vary the screw speed (output)
To move the mandrel of the die up and down, thereby decreasing and increasing the size of the gap.
with without
Extrusion blow moulding

## Slide 7
Extrusion blow moulding can be:
Continuous
Discontinuous or intermitted
Blow mould: usually made of Al; pressure is typically in the range of 0.4…0.8 MPa
Extrusion blow moulding

## Slide 8
Continuous blowing: a product with a small or medium volume in large-scale production. Short cycle time.
Max 1 l product size - mold lifting
Over 1 l product size – parision transfer
Mold lifting with continuous extrusion of the parison
Extrusion blow moulding
Extruder die
Blow mold
Parison
Extruder
1.Extrusion of parison
2. Mold closing
3. Blowing
4. Cooling
5. Ejection of part
6. Raising of mold
Flash
Pressurised air

## Slide 9
Mould shuttle with continuous extrusion of the parison
Extrusion blow moulding

## Slide 10
Vertical rotary wheel system with continuous extrusion of the parison
Extrusion blow moulding

## Slide 11
Blow molder with a rotating table
Extrusion blow moulding

## Slide 12
Parison transfer system with continuous extrusion of parison
Extrusion blow moulding

## Slide 13
Discontinuous or intermitted: for products with a larger volume (>5 l). Accumulator is used for storing the polymer melt. It is not suitable for heat-sensitive polymers
Extrusion blow moulding
Mandrel for thickness adjustment
Hidraulic slave cylinder
Ring piston
Melt from extruder
Moving moldhalf
Programmed insert
Parison

## Slide 14
Coextrusion die for parison-extrusion
e.g. PP, HDPE+EVOH (Ethylene-vinyl alcohol)
Low gas permeability
Extrusion blow moulding
Bottle wall thickness
Path of gas molecule
PP or HDPE
EVOH

## Slide 15
Recommended training videos (Paulson Training):
https://www.youtube.com/watch?v=oY7hyuMHm68&list=PLpL9tJRpo7WVrz7Ulb4PAjxrzkre84vQ6&index=1
https://www.youtube.com/watch?v=nSHOMBmpEyE&list=PLpL9tJRpo7WVrz7Ulb4PAjxrzkre84vQ6&index=2
https://www.youtube.com/watch?v=YWzaZYHXS9s&list=PLpL9tJRpo7WVrz7Ulb4PAjxrzkre84vQ6&index=3
https://www.youtube.com/watch?v=RDV6NXQ_7Rk&list=PLpL9tJRpo7WVrz7Ulb4PAjxrzkre84vQ6&index=6
Extrusion blow moulding

## Slide 16
Injection blow moulding

## Slide 17
https://youtu.be/pN-MWbcE_vM
Injection blow moulding:
The preform is produced by injection moulding, then the preform is blown in a closed mould
There is no flash (no waste), no welding line
Lower melt-strength materials can be processed (e.g. PS, PET)
Rotationally symmetric and oval products can be manufactured
Accurate wall thickness distribution, precious neck region
Crystallization can be controlled, so transparent products can be made
Max blowing index 3:1, ideal preform L/D 10:1, ideal preform wall thickness 2-5 mm
Major techniques:
Injection moulding and blowing on the same machine
Injection moulding and blow moulding on separate machines
+ Injection stretch blow moulding for both techniques above
Injection blow moulding

## Slide 18
Injection moulding and blowing on the same machine
Injection blow moulding

## Slide 19
Injection moulding and blow moulding on separate machines
Injection blow moulding
IM of preform Blowing of preform

## Slide 20
Injection stretch blow moulding
https://www.youtube.com/watch?v=NE4c1gwzPb4
Injection blow moulding
Biaxial stretching -> higher orientation -> higher mechanical strength
e.g. PET bottles: 3.8 circumferential and 2.8 longitudinal stretching -> 200 MPa and 100 MPa tensile strength respectively

## Slide 21
Injection stretch blow moulding:
For polyethylene terephthalate (PET) bottles
Goal of stretching: biaxial stretching, orientation
Molecular orientation improves mechanical properties (weaker, cheaper material OR smaller wall thickness is enough), gas permeability, gloss and transparency, dimensional accuracy.
PET – semi crystalline – how can it remain transparent?
Injection blow moulding
Injection molding: low injection speed -> no stress induced crystallization
Blow molding with stretching: preheating to 100 °C (Tg<Tmaterial<Tmelt)
only small crystals can form (no spherulite )
no refraction for smaller crystals than the wavelength of the visible light

## Slide 22
Injection blow moulding

## Slide 23
Blow moulds:
https://www.youtube.com/watch?v=ZfyPCujUPms
Injection blow moulding

## Slide 24
Rotational moulding

## Slide 25
Rotational moulding:
  https://www.youtube.com/watch?v=ZWvhvTXEUQ4
Biaxially rotating closed moulds
For preparing large products (1…10 m3)
There is no seam (weld line) no residual stress
Generally used materials:
  LLDPE, LDPE, HDPE
  PVC (powder, fluid)
  PP, rPP
  PA6
  PC
  Recommended videos:
  https://www.youtube.com/watch?v=ckN8Ot6lWRE
  https://www.youtube.com/watch?v=-d_cyeFXJWk&list=TLPQMDIxMTIwMjA1ZRpDXFpFlQ&index=3
  https://www.youtube.com/watch?v=lAQYfJAuw5M
Rotational moulding
  Other materials

## Slide 26
Requirements for the materials of rotational moulding
Powder (75…500 µm), ground material, viscous fluid, monomer, oligomer
Thermal stability
Particle size distribution (more even)
Sinterability of the particles
Properly high melt strength
Rotational moulding

## Slide 27
Examples:
Rotational moulding
LLDPE
LDPE
HDPE

## Slide 28
Examples:
Rotational moulding
PP
XLPE
PVC
PA
PC

## Slide 29
Principle:
Rotational moulding

## Slide 30
Biaxial rotation
Both in heating and cooling phases
Simultaneous rotation of both axes
Different rotational speed of the axes (the speed of the main axis is higher)
RPMs of the axes have to be different and must not be an integer multiple of each other (correct: 3.75:1)
Low revolution speed (˂30 rpm), mostly 3-10 rpm
Rotational moulding

## Slide 31
Process of the rotational moulding - heating
Rotational moulding

## Slide 32
Process of rotational moulding - heating
Rotational moulding

## Slide 33
Heating methods:
Hot air
Direct flame (gas combustion)
Molten salt
Steam
Infrared
Microwave
Hot water/oil
Rotational moulding

## Slide 34
Cooling
Mainly with cold air or water spray
The moulds are kept rotating biaxially
Depends on the materials (heat capacity)
Cooling time is proportional to the square of wall thickness
Shrinkage has to be considered
Removing the product is done manually
Followed by cutting, drilling, etc.
Rotational moulding

## Slide 35
Technological setup
Rotational moulding

## Slide 36
‚Rock and roll’ setup
Rotational moulding

## Slide 37
‚Clamshell’ setup
Rotational moulding

## Slide 38
Common arrangement of rotational moulding
Rotational moulding

## Slide 39
Rotation partly with the heating chamber
Rotational moulding

## Slide 40
Rotational mould:
Rotational moulding
Mould materials:
Steel
Al

## Slide 41
Rotational mould – cast Al:
Rotational moulding

## Slide 42
Rotational moulding

## Slide 43
Rotational moulding

## Slide 44
Based on the thermoforming technique: Two preforms (sheets) are formed simultaneously in the lower and the upper moulds and in the meantime the two halves (sheets during forming) are welded together with proper pressure
Mainly for large, flat, stiff, light products with different side colours or different materials (must be compatible)
Twin-sheet thermoforming

## Slide 45
Twin-sheet thermoforming

## Slide 46
Twin-sheet thermoforming

## Slide 47: Thank you for your attention!

## Slide 48
References
References:
J.R. Wagner Jr., E.M. Mount III, H.F. Giles Jr.: PDL Handbook Series, Extrusion: The Definitive Processing Guide and Handbook. Elsevier Inc., Oxford, 2014
D.V. Rosato, A.V. Rosato, D.P. DiMattia: Blow Molding Handbook. Hanser, Munich, 2004
G.L. Beall, J.L. Throne: Hollow Plastic Parts: Design and Manufacture. Hanser, Munich, 2004
C. Rauwendaal: Polymer Mixing: A Self-Study Guide. Hanser, Munich, 1998
J.L White, A.Y. Coran, A. Moet: Polymer Mixing: Technology and Engineering. Hanser, Munich, 2001
J.L. Throne: Technology of Thermoforming. Hanser, Munich, 1996
P. Schwarzmann: Thermoforming: A Practical Guide. Hanser, Munich, 2001
W. Michaeli: Plastic Processes: An Introduction. Hanser, Munich, 1995
C. A. Harper: Handbook of Plastic Processes. Wiley-Interscience, Hoboken, New Jersey, 2006